SPECIFICATIONS OF COBALT COATING BY BIPOLAR ELECTRONIC METHOD

Kuzevanova I.S. 1, Zulfigarov A.O. 1, Vlasenko N.E. 1, Kovalenko I.V. 1

1 National technical university of Ukraine “Igor Sikorskyi Kyiv Polytechnic Institute”; 37, Beresteysky Avenue, Kyiv, Ukraine, 03056

kuzevanova2009@ukr.net

The speed  of  the  electrochemical  process  of  metal application  is  determined  by  the  current  density, which  is  a  function  of  such  properties  as: composition  of  the  electrolyte,  temperature, circulation speed, electrode movement, and the other [1,2].

The study of the potential distribution,  the  influence of current density,   and other components of   the electrochemical process for monopolar (with current removal)  and bipolar  (without  current removal) electrodes.

Fig. 1. The dependence of potential distribution on the length of the wire - monopolar, at current density, А/dm2: 1 – 50, 2 – 60, 3 – 70, 4 – 80, 5 – 90

Here, the potential distribution along the length of the monopolar electrode is clearly presented. It is clearly seen that when moving away from the contact point, a uniform distribution of the potential occurs, which is associated with an increase in the resistance of the electrode - wire. Heating and metal overgrowing of the contact point - direct current to the wire.

- Bayrachny  B.I.,  Orekhov  V.V.  (1988). Spravochnik  gal'vanika  [The  reference  of  the galvanic]. Kharkov: Prapor, p.180.

- Yurtov E.V., Matveeva A.G. (2013). Shablon dlya     prigotovleniya     pokrytiya     iz nanostrukturirovannogo  nikelya  [Template  for  the production  of  nanostructured  nickel  coathing]. Chemistry technology, 14(1), pp. 24-29.